HOLLOWS

The inside diameter of our hollows is forged into the part rather than bored from a bar, which makes them an excellent option that eliminates extra time, cost and material waste. Since we forge them as a single component; we pass along several benefits to our customers by saving production time and increasing part strength.

MANUFACTURING CAPABILITIES

| Range | O.D. up to 60 in |
| --- | --- |
|  | I.D. up to 30 in |
|  | Weight up to 55,000 lb. |
| Material | Carbon Steel, Alloy Steel, Tool Steel, Stainless Steel. |
| Heat Treat | Normalizing, Quenching, Tempering, Annealing, Solution Annealing, Spherodizing, Aging, Stress Relieving. |
| Testing | Destructive and Non-Destructive. |
| Machining | Available CNC machining capabilities: vertical & horizontal turning, milling, boring, drilling, deep drilling. |

MATERIAL STOCKING GRADES

Classification

Carbon and Low

Alloy steels

Alloy Steels

Tool Steels

Stainless Steels

Superalloys

Aluminum

Titanium

Grade

A105

1010

1018

1020

1035

1045

1050

1080

1552

A350 Grade LF6

A350 Grade LF2

A694

4130

4140

4145

4320

4330

4340

52100

8620

8630

A182 Grade F5

A 182 Grade F11

A 182 Grade F22

A707 Grade L5

A707 Grade 3W

H13

P20

L6

A182 F44

A182 F51

A182 F53

A182 F60

A182 F91

15-5 PH

17-4 PH

304

304L

310

316

316L

321

347

410

420

422

431

F6NM

Alloy 718

Alloy 718 Plus

Waspaloy

Alloy 909

Alloy 907

Alloy 625

Alloy 600

Alloy 617

Alloy X

Alloy H230

Alloy 188

Alloy H242

Alloy HR120

Nimonic 80

Alloy 825

Alloy 800 H

Alloy C276

Monel 400

Alloy C263

Thermo Span

Al 6061

Al 7075

Al 2618

Al 2014

Al 2219

Al 7050

Ti-6-4

Ti 6-2-4-2

Ti 21s

Ti 834

Ti-407

UNS Number

K03504

G10100

G10180

G10200

G10350

G10450

G10500

G10800

G15520

K03011

G41300

G41400

G41450

G43200

G43400

G86200

G86300

K41545

K11597

K21590

T20813

T51620

T61206

S31254

S31803

S32750

S32205

K90901

S15500

S17400

S30400

S30403

S31000

S31600

S31603

S32100

S34700

S41000

S42000

S42200

S43100

S41500

N07718

N07001

N19909

N19907

N06625

N06600

N06617

N06002

N06230

R30188

N10242

N08120

N07080

N08825

N08800/N08810

N10276

N04400

N07263

S66286

N07041

R56400

R54620

R58210

DIN

C22.8

CK10

CK15

CK20

CK35

CK45

CK50

CK80

C22.8

E355

25CrMo4

42CrMo2

34CrNiMo6

100Cr6

21NiCrMo22

12CrMo195

13CrMo4-5

10CrMo9-10

X 40 CrMoV 5-1

40CrMnNiMo8-6-4

55NiCrMoV6

X1CrNiMoN20-18-7

X 2 CrNiMoN22-5-3

X2CrNiMoN25-7-4

X 10 CrMoVNb9-1

X5CrNiCuNb15-5

X5CrNiCuNb 17-4

X5CrNi18-10

X5CrNi18-9

X8 CrNi 25-21

X5CrNiMo17 12-2

X2CrNiMo17 12-2

X6CrNiTi18-10

X6CrNiNb18-10

X12Cr13

X46Cr13

X17CrNi16-2

X 22 CrNiMoV 12-1

X11CrMo 12-1

X 3 CrNiMo 13-4

NiCr19Fe19Nb5Mo3

NiCr20Co13Mo4Ti3Al

X4NiCo38Nb

X4NiCo38Nb

NiCr22Mo9Nb

NiCr15Fe8

NiCr23Co12Mo

NiCr22Fe18Mo

NiCo29Cr28Si

CoCr22NiW

NiFe33Cr25Co

NiCr20TiAl

NiCr 21 Mo

X8 NiCrAlTi 32-21

NiMo 16 Cr 15 W

NiCu 30 Fe

NiCo20Cr20Mo6Ti2Al

X5 NiCrTi 26-15

NiCr19Co11MoTi

TiAl6V4

TiAl6Sn2Zr4Mo2

Werkstoff Nr

1.0460

1.1121

1.1141

1.1181

1.1191

1.0460

1.0580

1.7218

1.7225

1.6582

1.3505

1.6543

1.6545

1.7362

1.7335

1.7380

1.2344

1.2311

1.2713

1.4547

1.4462

1.4410

1.4903

1.4545

1.4542

1.4301

1.4306

1.4845

1.4401

1.4404

1.4541

1.4551

1.4006

1.4034

1.4935

1.4057

1.4923

1.4313

2.4668

2.4654

2.4856

2.4816

2.4663

2.4665

2.4880

2.4683

2.4854

2.4952

2.4858

1.4876 / 1.4958

2.4819

2.4360

2.4650

1.4980

2.4973

3.7165

3.7145